University of jordan

School of engineering

Mechanical department

Strength lab report

Experiment #2

( torsion test )

Introduction :

When torsion is applied to a body , shear stresses will develop in that body (specimen) and as all kind of stresses it will cause deflection (strain) and may even cause failure of the material , that’s why it’s very important to study the behavior of different materials when they are under torsional loads .

This study is achieved through applying a “Torsion Test” to the material  , which is applied by putting a specimen under different values of torque and using the readings of these values with the angle of twist paired to each torque velue , these readings help us plotting the (shear stress-strain diagram) which we use to study the behavior and properties of that material under torsional loads .

Objective :

Studying the behavior of materials under torsion and obtaining some of there mechanical properties like : modulus of rigidity , modulus of resilience , modulus of rapture …etc.

Procedure :

1-take the dimentions of the specimen and specify the type of the material used

In our experiment we used two specimens : 1-brass (d=8mm , L=76.2mm)

2-steel (d=8mm , L=76.2mm)

2- locate the specimen between the loading device and the torque measuring device .

3-turn the handwheel to apply the torque and count after each full rotation (360degrees)

4-read out the torque value from the display of the amplifier (take the readings of each torque value with it’s indicated angle of twist)

In our experiment :

For steel 19 readings were taken .

For brass 181 readings were taken .

Apparatus :

*two specimens : (solid cylindrical)

1- steel specimen ( d=8mm , L=76.2mm)

2- brass specimen (d=mm , L=76.2mm)

*

Theory :

When a shaft is subjected to a torque or twisting a shearing stress is produced in the shaft. The shear stress varies from zero in the axis to a maximum at the outside surface of the shaft.

The shear stress in a solid circular shaft in a given position can be expressed as:

τ = T r / J                              (1)

where

τ = shear stress (Pa, psi)

T = twisting moment (Nm, in lb)

r = distance from center to stressed surface in the given position (m, in)

J = Polar Moment of Inertia of Area (m4, in4)

Note

- the "Polar Moment of Inertia of an Area" is a measure of a shaft's ability to resist torsion. The "Polar Moment of Inertia" is defined with respect to an axis perpendicular to the area considered. It is analogous to the "Area Moment of Inertia" - which characterizes a beam's ability to resist bending - required to predict deflection and stress in a beam.

"Polar Moment of Inertia of an Area" is also called "Polar Moment of Inertia", "Second Moment of Area", "Area Moment of Inertia", "Polar Moment of Area" or "Second Area Moment".

#### Polar Moment of Inertia vs. Area Moment of Inertia

- "Polar Moment of Inertia" - a measure of a beam's ability to resist torsion - which is required to calculate the twist of a beam subjected to torque

- "Area Moment of Inertia" - a property of shape that is used to predict deflection, bending and stress in beams

### Circular Shaft and Maximum Moment or Torque

Maximum moment in a circular shaft can be expressed as:

Tmax = τmax J / R                               (2)

where

Tmax = maximum twisting moment (Nm, in lb)

τmax = maximum shear stress (Pa, psi)

R = radius of shaft (m, in)

Combining (2) and (3) for a solid shaft

Tmax = (π / 16) τmax D3                            (2b)

Combining (2) and (3b) for a hollow shaft

Tmax = (π / 16) τmax (D4 - d4) / D                             (2c)

### Circular Shaft and Polar Moment of Inertia

Polar Moment of Inertia of a circular solid shaft can be expressed as

J = π R4 / 2

= π (D / 2)4 / 2

= π D4 / 32                          (3)

where

D = shaft outside diameter (m, in)

Polar Moment of Inertia of a circular hollow shaft can be expressed as

J = π (D4 - d4) / 32                          (3b)

where

d = shaft inside diameter (m, in)

### Diameter of a Solid Shaft

Diameter of a solid shaft can calculated by the formula

D = 1.72 (Tmax / τmax)1/3                            (4)

### Torsional Deflection of Shaft

The angular deflection of a torsion shaft can be expressed as

α = L T / (J G)                                  (5)

where

α = angular shaft deflection (radians)

L = length of shaft (m, in)

G = Shear Modulus of Rigidity - or Modulus of Rigidity (Pa, psi)

The angular deflection of a torsion solid shaft can be expressed as

α = 32 L T / (G π D4)                             (5a)

The angular deflection of a torsion hollow shaft can be expressed as

α = 32 L T / (G π (D4- d4))                              (5b)

The angle in degrees can be achieved by multiplying the angle θ in radians with 180 / π.

Solid shaft (π replaced)

αdegrees ≈ 584 L T / (G D4)                              (6a)

Hollow shaft (π replaced)

αdegrees ≈ 584 L T / (G (D4- d4)                            (6b)

raw data :

steel :

| no. of reading | applied torque (N.m) | input angle of twist (degrees) |
| --- | --- | --- |
| 1 | 0.05 | 360 |
| 2 | 0.85 | 720 |
| 3 | 3.6 | 1080 |
| 4 | 12.45 | 1440 |
| 5 | 21 | 1800 |
| 6 | 23.2 | 2160 |
| 7 | 24.3 | 2520 |
| 8 | 24.85 | 2880 |
| 9 | 25.15 | 3240 |
| 10 | 25.4 | 3600 |
| 11 | 25.45 | 3960 |
| 12 | 25.55 | 4320 |
| 13 | 25.6 | 4680 |
| 14 | 25.6 | 5040 |
| 15 | 25.6 | 5400 |
| 16 | 25.6 | 5760 |
| 17 | 25.55 | 6120 |
| 18 | 24.55 | 6480 |
| 19 | 21.5 | 6840 |
| 20 | 12 | 7200 |

Brass :

| no. of reading | applied torque(N.m) | input angle of twist (degrees) |
| --- | --- | --- |
| 1 | 0.15 | 360 |
| 2 | 0.2 | 720 |
| 3 | 5.25 | 1080 |
| 4 | 6.95 | 1440 |
| 5 | 8.1 | 1800 |
| 6 | 8.6 | 2160 |
| 7 | 9.05 | 2520 |
| 8 | 9.35 | 2880 |
| 9 | 9.5 | 3240 |
| 10 | 9.65 | 3600 |
| 11 | 9.8 | 3960 |
| 12 | 9.9 | 4320 |
| 13 | 10 | 4680 |
| 14 | 10.1 | 5040 |
| 15 | 10.25 | 5400 |
| 16 | 10.3 | 5760 |
| 17 | 10.4 | 6120 |
| 18 | 10.35 | 6480 |
| 19 | 10.4 | 6840 |
| 20 | 10.5 | 7200 |
| 21 | 10.55 | 7560 |
| 22 | 10.6 | 7920 |
| 23 | 10.65 | 8280 |
| 24 | 10.75 | 8640 |
| 25 | 10.8 | 9000 |
| 26 | 10.85 | 9360 |
| 27 | 10.9 | 9720 |
| 28 | 10.95 | 10080 |
| 29 | 11 | 10440 |
| 30 | 11.1 | 10800 |
| 31 | 11.15 | 11160 |
| 32 | 11.2 | 11520 |
| 33 | 11.25 | 11880 |
| 34 | 11.3 | 12240 |
| 35 | 11.35 | 12600 |
| 36 | 11.4 | 12960 |
| 37 | 11.45 | 13320 |
| 38 | 11.5 | 13680 |
| 39 | 11.55 | 14040 |
| 40 | 11.55 | 14400 |
| 41 | 11.6 | 14760 |
| 42 | 11.65 | 15120 |
| 43 | 11.65 | 15480 |
| 44 | 11.7 | 15840 |
| 45 | 11.75 | 16200 |
| 46 | 11.75 | 16560 |
| 47 | 11.8 | 16920 |
| 48 | 11.85 | 17280 |
| 49 | 11.9 | 17640 |
| 50 | 11.9 | 18000 |
| 51 | 11.95 | 18360 |
| 52 | 12 | 18720 |
| 53 | 12.05 | 19080 |
| 54 | 12.05 | 19440 |
| 55 | 12.1 | 19800 |
| 56 | 12.1 | 20160 |
| 57 | 12.15 | 20520 |
| 58 | 12.2 | 20880 |
| 59 | 12.25 | 21240 |
| 60 | 12.25 | 21600 |
| 61 | 12.3 | 21960 |
| 62 | 12.3 | 22320 |
| 63 | 12.35 | 22680 |
| 64 | 12.4 | 23040 |
| 65 | 12.4 | 23400 |
| 66 | 12.45 | 23760 |
| 67 | 12.5 | 24120 |
| 68 | 12.5 | 24480 |
| 69 | 12.5 | 24840 |
| 70 | 12.55 | 25200 |
| 71 | 12.6 | 25560 |
| 72 | 12.6 | 25920 |
| 73 | 12.65 | 26280 |
| 74 | 12.7 | 26640 |
| 75 | 12.7 | 27000 |
| 76 | 12.75 | 27360 |
| 77 | 12.75 | 27720 |
| 78 | 12.8 | 28080 |
| 79 | 12.85 | 28440 |
| 80 | 12.85 | 28800 |
| 81 | 12.9 | 29160 |
| 82 | 12.9 | 29520 |
| 83 | 13.05 | 29880 |
| 84 | 13.1 | 30240 |
| 85 | 13.1 | 30600 |
| 86 | 13.15 | 30960 |
| 87 | 13.15 | 31320 |
| 88 | 13.2 | 31680 |
| 89 | 13.2 | 32040 |
| 90 | 13.25 | 32400 |
| 91 | 13.3 | 32760 |
| 92 | 13.3 | 33120 |
| 93 | 13.35 | 33480 |
| 94 | 13.35 | 33840 |
| 95 | 13.4 | 34200 |
| 96 | 13.4 | 34560 |
| 97 | 13.45 | 34920 |
| 98 | 13.45 | 35280 |
| 99 | 13.5 | 35640 |
| 100 | 13.5 | 36000 |
| 101 | 13.5 | 36360 |
| 102 | 13.55 | 36720 |
| 103 | 13.6 | 37080 |
| 104 | 13.6 | 37440 |
| 105 | 13.6 | 37800 |
| 106 | 13.65 | 38160 |
| 107 | 13.65 | 38520 |
| 108 | 13.7 | 38880 |
| 109 | 13.7 | 39240 |
| 110 | 13.7 | 39600 |
| 111 | 13.75 | 39960 |
| 112 | 13.75 | 40320 |
| 113 | 13.8 | 40680 |
| 114 | 13.8 | 41040 |
| 115 | 13.8 | 41400 |
| 116 | 13.85 | 41760 |
| 117 | 13.85 | 42120 |
| 118 | 13.9 | 42480 |
| 119 | 13.9 | 42840 |
| 120 | 13.9 | 43200 |
| 121 | 13.95 | 43560 |
| 122 | 13.95 | 43920 |
| 123 | 13.95 | 44280 |
| 124 | 14 | 44640 |
| 125 | 14.05 | 45000 |
| 126 | 14.05 | 45360 |
| 127 | 14.1 | 45720 |
| 128 | 14.15 | 46080 |
| 129 | 14.15 | 46440 |
| 130 | 14.2 | 46800 |
| 131 | 14.2 | 47160 |
| 132 | 14.2 | 47520 |
| 133 | 14.25 | 47880 |
| 134 | 14.25 | 48240 |
| 135 | 14.3 | 48600 |
| 136 | 14.3 | 48960 |
| 137 | 14.3 | 49320 |
| 138 | 14.35 | 49680 |
| 139 | 14.35 | 50040 |
| 140 | 14.4 | 50400 |
| 141 | 14.4 | 50760 |
| 142 | 14.4 | 51120 |
| 143 | 14.4 | 51480 |
| 144 | 14.4 | 51840 |
| 145 | 14.45 | 52200 |
| 146 | 14.5 | 52560 |
| 147 | 14.5 | 52920 |
| 148 | 14.5 | 53280 |
| 149 | 14.55 | 53640 |
| 150 | 14.55 | 54000 |
| 151 | 14.55 | 54360 |
| 152 | 14.6 | 54720 |
| 153 | 14.6 | 55080 |
| 154 | 14.6 | 55440 |
| 155 | 14.6 | 55800 |
| 156 | 14.65 | 56160 |
| 157 | 14.65 | 56520 |
| 158 | 14.65 | 56880 |
| 159 | 14.65 | 57240 |
| 160 | 14.7 | 57600 |
| 161 | 14.7 | 57960 |
| 162 | 14.7 | 58320 |
| 163 | 14.75 | 58680 |
| 164 | 14.75 | 59040 |
| 165 | 14.75 | 59400 |
| 166 | 14.75 | 59760 |
| 167 | 14.75 | 60120 |
| 168 | 14.8 | 60480 |
| 169 | 14.8 | 60840 |
| 170 | 14.8 | 61200 |
| 171 | 14.8 | 61560 |
| 172 | 14.85 | 61920 |
| 173 | 14.8 | 62280 |
| 174 | 14.85 | 62640 |
| 175 | 14.9 | 63000 |
| 176 | 14.9 | 63360 |
| 177 | 14.9 | 63720 |
| 178 | 14.9 | 64080 |
| 179 | 14.95 | 64440 |
| 180 | 13.04 | 64800 |

Sample calculation :

For reading no.5 :

D=8mm , L=76.2mm

Input angle of twist Ø  = 5*360 = 1800

Applied torque =

Output angle of twist Ø  = Ø62=180062=29.0323 deg

Output angle of twist (rad/m) = Øoutput*π18076.2*10-3=29.0323*π1800.0762 = 6.6497 rad/m

Shear stress τ = 16*Td3*π=16*210.0083*π=  208890862.8 Pa = 208 Mpa

Shear strain ε = Ø outpu*RL =6.6497*0.004=0.026599 rad

Requirements :

Steel :

*shearing proportional limit : 210 MPa

*yield strength at an offset 0.1% : 225 MPa

*modulus of rigidity : 225*10^6/

*modulus of resilience :

*Modulus of rupture :

*total angle of twist : 20/62 = 0.32 rotations

Brass :

*shearing proportional limit : 890 MPa

*yield strength at an offset 0.1% : 920 MPa

*modulus of rigidity :

*modulus of resilience :

*Modulus of rupture :

*Total angle of twist: 180/62 = 2.9 rotations

Discussion and conclusion :

- Advantages and disadvantages of tubular and solid cylindrical torsional specimens

Advantages :

(a) accurate shear strain measurement may be obtained because of the long gage section that this type of specimen has;

(b) accurate strain measurements may be obtained in axial and hoop strains

(c) the specimen may be used for combined axial-torsional testing

(d) the specimen is suitable for test involving unloading/reloading/cyclic loading

(e) the specimen may be used for investigation of shear band localization.

Disadvantages :

The specimen might be non-homogeneous which causes errors and false-readings

- The results shows that steel can’t take high values of torque before fracture compared to brass

Reduced data :

Steel :

| no. of reading | applied torque (N.m) | input angle of twist (degrees) | output angle of twist (degrees) | output angle of twist (rad/m length) | shear stress(Mpa) | shear strain (rad) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.05 | 360 | 5.806452 | 0.132994 | 497359.2056 | 0.000305 |
| 2 | 0.85 | 720 | 11.6129 | 0.265989 | 8455106.496 | 0.00061 |
| 3 | 3.6 | 1080 | 17.41935 | 0.398983 | 35809862.81 | 0.000914 |
| 4 | 12.45 | 1440 | 23.22581 | 0.531977 | 123842442.2 | 0.001219 |
| 5 | 21 | 1800 | 29.03226 | 0.664972 | 208890866.4 | 0.001524 |
| 6 | 23.2 | 2160 | 34.83871 | 0.797966 | 230774671.4 | 0.001829 |
| 7 | 24.3 | 2520 | 40.64516 | 0.93096 | 241716573.9 | 0.002134 |
| 8 | 24.85 | 2880 | 46.45161 | 1.063955 | 247187525.2 | 0.002438 |
| 9 | 25.15 | 3240 | 52.25806 | 1.196949 | 250171680.4 | 0.002743 |
| 10 | 25.4 | 3600 | 58.06452 | 1.329944 | 252658476.5 | 0.003048 |
| 11 | 25.45 | 3960 | 63.87097 | 1.462938 | 253155835.7 | 0.003353 |
| 12 | 25.55 | 4320 | 69.67742 | 1.595932 | 254150554.1 | 0.003658 |
| 13 | 25.6 | 4680 | 75.48387 | 1.728927 | 254647913.3 | 0.003962 |
| 14 | 25.6 | 5040 | 81.29032 | 1.861921 | 254647913.3 | 0.004267 |
| 15 | 25.6 | 5400 | 87.09677 | 1.994915 | 254647913.3 | 0.004572 |
| 16 | 25.6 | 5760 | 92.90323 | 2.12791 | 254647913.3 | 0.004877 |
| 17 | 25.55 | 6120 | 98.70968 | 2.260904 | 254150554.1 | 0.005182 |
| 18 | 24.55 | 6480 | 104.5161 | 2.393898 | 244203370 | 0.005486 |
| 19 | 21.5 | 6840 | 110.3226 | 2.526893 | 213864458.4 | 0.005791 |
| 20 | 12 | 7200 | 116.129 | 2.659887 | 119366209.4 | 0.006096 |

Stress-strain curve

Torque-angle of twist curve

Brass  :

| no. of reading | applied torque(N.m) | input angle of twist (degrees) | output angle of twist | output of angle twist (rad/m length) | shear stress(Mpa) | shear strain(rad) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.15 | 360 | 5.806452 | 0.132994 | 14726215.3 | 0.000305 |
| 2 | 0.2 | 720 | 11.6129 | 0.265989 | 19634953.8 | 0.00061 |
| 3 | 5.25 | 1080 | 17.41935 | 0.398983 | 515417536 | 0.000914 |
| 4 | 6.95 | 1440 | 23.22581 | 0.531977 | 682314643 | 0.001219 |
| 5 | 8.1 | 1800 | 29.03226 | 0.664972 | 795215627 | 0.001524 |
| 6 | 8.6 | 2160 | 34.83871 | 0.797966 | 844303011 | 0.001829 |
| 7 | 9.05 | 2520 | 40.64516 | 0.93096 | 888481657 | 0.002134 |
| 8 | 9.35 | 2880 | 46.45161 | 1.063955 | 917934088 | 0.002438 |
| 9 | 9.5 | 3240 | 52.25806 | 1.196949 | 932660303 | 0.002743 |
| 10 | 9.65 | 3600 | 58.06452 | 1.329943 | 947386518 | 0.003048 |
| 11 | 9.8 | 3960 | 63.87097 | 1.462938 | 962112734 | 0.003353 |
| 12 | 9.9 | 4320 | 69.67742 | 1.595932 | 971930211 | 0.003658 |
| 13 | 10 | 4680 | 75.48387 | 1.728926 | 981747688 | 0.003962 |
| 14 | 10.1 | 5040 | 81.29032 | 1.861921 | 991565164 | 0.004267 |
| 15 | 10.25 | 5400 | 87.09677 | 1.994915 | 1006291380 | 0.004572 |
| 16 | 10.3 | 5760 | 92.90323 | 2.127909 | 1011200118 | 0.004877 |
| 17 | 10.4 | 6120 | 98.70968 | 2.260904 | 1021017595 | 0.005182 |
| 18 | 10.35 | 6480 | 104.5161 | 2.393898 | 1016108857 | 0.005486 |
| 19 | 10.4 | 6840 | 110.3226 | 2.526892 | 1021017595 | 0.005791 |
| 20 | 10.5 | 7200 | 116.129 | 2.659887 | 1030835072 | 0.006096 |
| 21 | 10.55 | 7560 | 121.9355 | 2.792881 | 1035743810 | 0.006401 |
| 22 | 10.6 | 7920 | 127.7419 | 2.925875 | 1040652549 | 0.006706 |
| 23 | 10.65 | 8280 | 133.5484 | 3.05887 | 1045561287 | 0.00701 |
| 24 | 10.75 | 8640 | 139.3548 | 3.191864 | 1055378764 | 0.007315 |
| 25 | 10.8 | 9000 | 145.1613 | 3.324858 | 1060287503 | 0.00762 |
| 26 | 10.85 | 9360 | 150.9677 | 3.457853 | 1065196241 | 0.007925 |
| 27 | 10.9 | 9720 | 156.7742 | 3.590847 | 1070104979 | 0.00823 |
| 28 | 10.95 | 10080 | 162.5806 | 3.723841 | 1075013718 | 0.008534 |
| 29 | 11 | 10440 | 168.3871 | 3.856836 | 1079922456 | 0.008839 |
| 30 | 11.1 | 10800 | 174.1935 | 3.98983 | 1089739933 | 0.009144 |
| 31 | 11.15 | 11160 | 180 | 4.122824 | 1094648672 | 0.009449 |
| 32 | 11.2 | 11520 | 185.8065 | 4.255819 | 1099557410 | 0.009754 |
| 33 | 11.25 | 11880 | 191.6129 | 4.388813 | 1104466148 | 0.010058 |
| 34 | 11.3 | 12240 | 197.4194 | 4.521807 | 1109374887 | 0.010363 |
| 35 | 11.35 | 12600 | 203.2258 | 4.654802 | 1114283625 | 0.010668 |
| 36 | 11.4 | 12960 | 209.0323 | 4.787796 | 1119192364 | 0.010973 |
| 37 | 11.45 | 13320 | 214.8387 | 4.92079 | 1124101102 | 0.011278 |
| 38 | 11.5 | 13680 | 220.6452 | 5.053785 | 1129009841 | 0.011582 |
| 39 | 11.55 | 14040 | 226.4516 | 5.186779 | 1133918579 | 0.011887 |
| 40 | 11.55 | 14400 | 232.2581 | 5.319773 | 1133918579 | 0.012192 |
| 41 | 11.6 | 14760 | 238.0645 | 5.452768 | 1138827318 | 0.012497 |
| 42 | 11.65 | 15120 | 243.871 | 5.585762 | 1143736056 | 0.012802 |
| 43 | 11.65 | 15480 | 249.6774 | 5.718756 | 1143736056 | 0.013106 |
| 44 | 11.7 | 15840 | 255.4839 | 5.851751 | 1148644794 | 0.013411 |
| 45 | 11.75 | 16200 | 261.2903 | 5.984745 | 1153553533 | 0.013716 |
| 46 | 11.75 | 16560 | 267.0968 | 6.117739 | 1153553533 | 0.014021 |
| 47 | 11.8 | 16920 | 272.9032 | 6.250734 | 1158462271 | 0.014326 |
| 48 | 11.85 | 17280 | 278.7097 | 6.383728 | 1163371010 | 0.01463 |
| 49 | 11.9 | 17640 | 284.5161 | 6.516722 | 1168279748 | 0.014935 |
| 50 | 11.9 | 18000 | 290.3226 | 6.649717 | 1168279748 | 0.01524 |
| 51 | 11.95 | 18360 | 296.129 | 6.782711 | 1173188487 | 0.015545 |
| 52 | 12 | 18720 | 301.9355 | 6.915705 | 1178097225 | 0.01585 |
| 53 | 12.05 | 19080 | 307.7419 | 7.0487 | 1183005963 | 0.016154 |
| 54 | 12.05 | 19440 | 313.5484 | 7.181694 | 1183005963 | 0.016459 |
| 55 | 12.1 | 19800 | 319.3548 | 7.314688 | 1187914702 | 0.016764 |
| 56 | 12.1 | 20160 | 325.1613 | 7.447683 | 1187914702 | 0.017069 |
| 57 | 12.15 | 20520 | 330.9677 | 7.580677 | 1192823440 | 0.017374 |
| 58 | 12.2 | 20880 | 336.7742 | 7.713671 | 1197732179 | 0.017678 |
| 59 | 12.25 | 21240 | 342.5806 | 7.846666 | 1202640917 | 0.017983 |
| 60 | 12.25 | 21600 | 348.3871 | 7.97966 | 1202640917 | 0.018288 |
| 61 | 12.3 | 21960 | 354.1935 | 8.112654 | 1207549656 | 0.018593 |
| 62 | 12.3 | 22320 | 360 | 8.245649 | 1207549656 | 0.018898 |
| 63 | 12.35 | 22680 | 365.8065 | 8.378643 | 1212458394 | 0.019202 |
| 64 | 12.4 | 23040 | 371.6129 | 8.511637 | 1217367133 | 0.019507 |
| 65 | 12.4 | 23400 | 377.4194 | 8.644632 | 1217367133 | 0.019812 |
| 66 | 12.45 | 23760 | 383.2258 | 8.777626 | 1222275871 | 0.020117 |
| 67 | 12.5 | 24120 | 389.0323 | 8.91062 | 1227184609 | 0.020422 |
| 68 | 12.5 | 24480 | 394.8387 | 9.043615 | 1227184609 | 0.020726 |
| 69 | 12.5 | 24840 | 400.6452 | 9.176609 | 1227184609 | 0.021031 |
| 70 | 12.55 | 25200 | 406.4516 | 9.309604 | 1232093348 | 0.021336 |
| 71 | 12.6 | 25560 | 412.2581 | 9.442598 | 1237002086 | 0.021641 |
| 72 | 12.6 | 25920 | 418.0645 | 9.575592 | 1237002086 | 0.021946 |
| 73 | 12.65 | 26280 | 423.871 | 9.708587 | 1241910825 | 0.02225 |
| 74 | 12.7 | 26640 | 429.6774 | 9.841581 | 1246819563 | 0.022555 |
| 75 | 12.7 | 27000 | 435.4839 | 9.974575 | 1246819563 | 0.02286 |
| 76 | 12.75 | 27360 | 441.2903 | 10.10757 | 1251728302 | 0.023165 |
| 77 | 12.75 | 27720 | 447.0968 | 10.24056 | 1251728302 | 0.02347 |
| 78 | 12.8 | 28080 | 452.9032 | 10.37356 | 1256637040 | 0.023774 |
| 79 | 12.85 | 28440 | 458.7097 | 10.50655 | 1261545778 | 0.024079 |
| 80 | 12.85 | 28800 | 464.5161 | 10.63955 | 1261545778 | 0.024384 |
| 81 | 12.9 | 29160 | 470.3226 | 10.77254 | 1266454517 | 0.024689 |
| 82 | 12.9 | 29520 | 476.129 | 10.90554 | 1266454517 | 0.024994 |
| 83 | 13.05 | 29880 | 481.9355 | 11.03853 | 1281180732 | 0.025298 |
| 84 | 13.1 | 30240 | 487.7419 | 11.17152 | 1286089471 | 0.025603 |
| 85 | 13.1 | 30600 | 493.5484 | 11.30452 | 1286089471 | 0.025908 |
| 86 | 13.15 | 30960 | 499.3548 | 11.43751 | 1290998209 | 0.026213 |
| 87 | 13.15 | 31320 | 505.1613 | 11.57051 | 1290998209 | 0.026518 |
| 88 | 13.2 | 31680 | 510.9677 | 11.7035 | 1295906948 | 0.026822 |
| 89 | 13.2 | 32040 | 516.7742 | 11.8365 | 1295906948 | 0.027127 |
| 90 | 13.25 | 32400 | 522.5806 | 11.96949 | 1300815686 | 0.027432 |
| 91 | 13.3 | 32760 | 528.3871 | 12.10248 | 1305724424 | 0.027737 |
| 92 | 13.3 | 33120 | 534.1935 | 12.23548 | 1305724424 | 0.028042 |
| 93 | 13.35 | 33480 | 540 | 12.36847 | 1310633163 | 0.028346 |
| 94 | 13.35 | 33840 | 545.8065 | 12.50147 | 1310633163 | 0.028651 |
| 95 | 13.4 | 34200 | 551.6129 | 12.63446 | 1315541901 | 0.028956 |
| 96 | 13.4 | 34560 | 557.4194 | 12.76746 | 1315541901 | 0.029261 |
| 97 | 13.45 | 34920 | 563.2258 | 12.90045 | 1320450640 | 0.029566 |
| 98 | 13.45 | 35280 | 569.0323 | 13.03344 | 1320450640 | 0.02987 |
| 99 | 13.5 | 35640 | 574.8387 | 13.16644 | 1325359378 | 0.030175 |
| 100 | 13.5 | 36000 | 580.6452 | 13.29943 | 1325359378 | 0.03048 |
| 101 | 13.5 | 36360 | 586.4516 | 13.43243 | 1325359378 | 0.030785 |
| 102 | 13.55 | 36720 | 592.2581 | 13.56542 | 1330268117 | 0.03109 |
| 103 | 13.6 | 37080 | 598.0645 | 13.69842 | 1335176855 | 0.031394 |
| 104 | 13.6 | 37440 | 603.871 | 13.83141 | 1335176855 | 0.031699 |
| 105 | 13.6 | 37800 | 609.6774 | 13.96441 | 1335176855 | 0.032004 |
| 106 | 13.65 | 38160 | 615.4839 | 14.0974 | 1340085593 | 0.032309 |
| 107 | 13.65 | 38520 | 621.2903 | 14.23039 | 1340085593 | 0.032614 |
| 108 | 13.7 | 38880 | 627.0968 | 14.36339 | 1344994332 | 0.032918 |
| 109 | 13.7 | 39240 | 632.9032 | 14.49638 | 1344994332 | 0.033223 |
| 110 | 13.7 | 39600 | 638.7097 | 14.62938 | 1344994332 | 0.033528 |
| 111 | 13.75 | 39960 | 644.5161 | 14.76237 | 1349903070 | 0.033833 |
| 112 | 13.75 | 40320 | 650.3226 | 14.89537 | 1349903070 | 0.034138 |
| 113 | 13.8 | 40680 | 656.129 | 15.02836 | 1354811809 | 0.034442 |
| 114 | 13.8 | 41040 | 661.9355 | 15.16135 | 1354811809 | 0.034747 |
| 115 | 13.8 | 41400 | 667.7419 | 15.29435 | 1354811809 | 0.035052 |
| 116 | 13.85 | 41760 | 673.5484 | 15.42734 | 1359720547 | 0.035357 |
| 117 | 13.85 | 42120 | 679.3548 | 15.56034 | 1359720547 | 0.035662 |
| 118 | 13.9 | 42480 | 685.1613 | 15.69333 | 1364629286 | 0.035966 |
| 119 | 13.9 | 42840 | 690.9677 | 15.82633 | 1364629286 | 0.036271 |
| 120 | 13.9 | 43200 | 696.7742 | 15.95932 | 1364629286 | 0.036576 |
| 121 | 13.95 | 43560 | 702.5806 | 16.09231 | 1369538024 | 0.036881 |
| 122 | 13.95 | 43920 | 708.3871 | 16.22531 | 1369538024 | 0.037186 |
| 123 | 13.95 | 44280 | 714.1935 | 16.3583 | 1369538024 | 0.03749 |
| 124 | 14 | 44640 | 720 | 16.4913 | 1374446763 | 0.037795 |
| 125 | 14.05 | 45000 | 725.8065 | 16.62429 | 1379355501 | 0.0381 |
| 126 | 14.05 | 45360 | 731.6129 | 16.75729 | 1379355501 | 0.038405 |
| 127 | 14.1 | 45720 | 737.4194 | 16.89028 | 1384264239 | 0.03871 |
| 128 | 14.15 | 46080 | 743.2258 | 17.02327 | 1389172978 | 0.039014 |
| 129 | 14.15 | 46440 | 749.0323 | 17.15627 | 1389172978 | 0.039319 |
| 130 | 14.2 | 46800 | 754.8387 | 17.28926 | 1394081716 | 0.039624 |
| 131 | 14.2 | 47160 | 760.6452 | 17.42226 | 1394081716 | 0.039929 |
| 132 | 14.2 | 47520 | 766.4516 | 17.55525 | 1394081716 | 0.040234 |
| 133 | 14.25 | 47880 | 772.2581 | 17.68825 | 1398990455 | 0.040538 |
| 134 | 14.25 | 48240 | 778.0645 | 17.82124 | 1398990455 | 0.040843 |
| 135 | 14.3 | 48600 | 783.871 | 17.95424 | 1403899193 | 0.041148 |
| 136 | 14.3 | 48960 | 789.6774 | 18.08723 | 1403899193 | 0.041453 |
| 137 | 14.3 | 49320 | 795.4839 | 18.22022 | 1403899193 | 0.041758 |
| 138 | 14.35 | 49680 | 801.2903 | 18.35322 | 1408807932 | 0.042062 |
| 139 | 14.35 | 50040 | 807.0968 | 18.48621 | 1408807932 | 0.042367 |
| 140 | 14.4 | 50400 | 812.9032 | 18.61921 | 1413716670 | 0.042672 |
| 141 | 14.4 | 50760 | 818.7097 | 18.7522 | 1413716670 | 0.042977 |
| 142 | 14.4 | 51120 | 824.5161 | 18.8852 | 1413716670 | 0.043282 |
| 143 | 14.4 | 51480 | 830.3226 | 19.01819 | 1413716670 | 0.043586 |
| 144 | 14.4 | 51840 | 836.129 | 19.15118 | 1413716670 | 0.043891 |
| 145 | 14.45 | 52200 | 841.9355 | 19.28418 | 1418625408 | 0.044196 |
| 146 | 14.5 | 52560 | 847.7419 | 19.41717 | 1423534147 | 0.044501 |
| 147 | 14.5 | 52920 | 853.5484 | 19.55017 | 1423534147 | 0.044806 |
| 148 | 14.5 | 53280 | 859.3548 | 19.68316 | 1423534147 | 0.04511 |
| 149 | 14.55 | 53640 | 865.1613 | 19.81616 | 1428442885 | 0.045415 |
| 150 | 14.55 | 54000 | 870.9677 | 19.94915 | 1428442885 | 0.04572 |
| 151 | 14.55 | 54360 | 876.7742 | 20.08214 | 1428442885 | 0.046025 |
| 152 | 14.6 | 54720 | 882.5806 | 20.21514 | 1433351624 | 0.04633 |
| 153 | 14.6 | 55080 | 888.3871 | 20.34813 | 1433351624 | 0.046634 |
| 154 | 14.6 | 55440 | 894.1935 | 20.48113 | 1433351624 | 0.046939 |
| 155 | 14.6 | 55800 | 900 | 20.61412 | 1433351624 | 0.047244 |
| 156 | 14.65 | 56160 | 905.8065 | 20.74712 | 1438260362 | 0.047549 |
| 157 | 14.65 | 56520 | 911.6129 | 20.88011 | 1438260362 | 0.047854 |
| 158 | 14.65 | 56880 | 917.4194 | 21.01311 | 1438260362 | 0.048158 |
| 159 | 14.65 | 57240 | 923.2258 | 21.1461 | 1438260362 | 0.048463 |
| 160 | 14.7 | 57600 | 929.0323 | 21.27909 | 1443169101 | 0.048768 |
| 161 | 14.7 | 57960 | 934.8387 | 21.41209 | 1443169101 | 0.049073 |
| 162 | 14.7 | 58320 | 940.6452 | 21.54508 | 1443169101 | 0.049378 |
| 163 | 14.75 | 58680 | 946.4516 | 21.67808 | 1448077839 | 0.049682 |
| 164 | 14.75 | 59040 | 952.2581 | 21.81107 | 1448077839 | 0.049987 |
| 165 | 14.75 | 59400 | 958.0645 | 21.94407 | 1448077839 | 0.050292 |
| 166 | 14.75 | 59760 | 963.871 | 22.07706 | 1448077839 | 0.050597 |
| 167 | 14.75 | 60120 | 969.6774 | 22.21005 | 1448077839 | 0.050902 |
| 168 | 14.8 | 60480 | 975.4839 | 22.34305 | 1452986578 | 0.051207 |
| 169 | 14.8 | 60840 | 981.2903 | 22.47604 | 1452986578 | 0.051511 |
| 170 | 14.8 | 61200 | 987.0968 | 22.60904 | 1452986578 | 0.051816 |
| 171 | 14.8 | 61560 | 992.9032 | 22.74203 | 1452986578 | 0.052121 |
| 172 | 14.85 | 61920 | 998.7097 | 22.87503 | 1457895316 | 0.052426 |
| 173 | 14.8 | 62280 | 1004.516 | 23.00802 | 1452986578 | 0.052731 |
| 174 | 14.85 | 62640 | 1010.323 | 23.14101 | 1457895316 | 0.053035 |
| 175 | 14.9 | 63000 | 1016.129 | 23.27401 | 1462804054 | 0.05334 |
| 176 | 14.9 | 63360 | 1021.935 | 23.407 | 1462804054 | 0.053645 |
| 177 | 14.9 | 63720 | 1027.742 | 23.54 | 1462804054 | 0.05395 |
| 178 | 14.9 | 64080 | 1033.548 | 23.67299 | 1462804054 | 0.054255 |
| 179 | 14.95 | 64440 | 1039.355 | 23.80599 | 1467712793 | 0.054559 |
| 180 | 13.04 | 64800 | 1045.161 | 23.93898 | 1280198985 | 0.054864 |

Stress-strain curve

Torque-angle of twist curve